DOW LATEX 470

Dow Latex 470 is a  styrene/butadiene latex specifically designed for use in cement mortars. DL 470 modified mortars exhibit greatly improved bond, tensile and flexural strength, and durability.  DL 470 contains an antifoam and specific additives to aid workability.  DL 470 may be added at levels of 6 to 12%(dry latex on cement) for mortars and up to 20% for high performance surfacing.

PROPERTIES	TYPICAL VALUE

Solids content	45 - 47.0%

pH	8.5 - 11.5

particle size	155 - 185 nm

stabilizer type	anionic

glass transition                             +8C

minimum film	6°C

forming temperature